# Moplen RP348R

### Polypropylene, Random Copolymer

## Product Description

"Moplen" RP348R is a nucleated and antistatic additivated random copolymer for injection moulding that displays excellent transparency combined with good flowability.

The main applications of "Moplen" RP348R are housewares and caps & closures.

## Product Characteristics

| Status | Commercial: Active |
| --- | --- |
| Test Method used | ISO ASTM |
| Availability | Europe, Africa-Middle East |
| Processing Method | Injection Moulding |
| Features | Antistatic, Clarity, High, Copolymer, Random, Flow, Good, Nucleated |
| Typical Customer Applications | Injection Moulded Caps and Closures, Housewares |

| Typical Properties | Method | Value | Unit |
| --- | --- | --- | --- |
| Physical |
| Density | ISO 1183 | 0.900 | g/cm³ |
| Melt flow rate (MFR) (230°C/2.16Kg) | ISO 1133 | 23 | g/10 min |
| Melt volume flow rate (230°C/2.16Kg) | ISO 1133 | 31.0 | cm³/10min |
| Mechanical |
| Tensile Modulus | ISO 527-1, -2 | 1100 | MPa |
| Tensile Stress at Yield | ISO 527-1, -2 | 29.0 | MPa |
| Tensile Strain at Break | ISO 527-1, -2 | >50 | % |
| Tensile Strain at Yield | ISO 527-1, -2 | 11 | % |
| Impact |
| Charpy unnotched impact strength | ISO 179 |  |  |
| (23 °C, Type 1, Edgewise) |  | 70.0 | kJ/m² |
| (0 °C, Type 1, Edgewise) |  | 200 | kJ/m² |
| Charpy notched impact strength | ISO 179 |  |  |
| (23 °C, Type 1, Edgewise, Notch A) |  | 6.00 | kJ/m² |
| (0 °C, Type 1, Edgewise, Notch A) |  | 3.00 | kJ/m² |
| Hardness |
| Ball indentation hardness | ISO 2039-1 | 60.0 | MPa |
| Notes |
| Typical properties; not to be construed as specifications. |

© 2003 Basell Service Company B.V. For the contact details of the Basell company selling this product in your country, please visit the Basell website at www.basell.com. Before using a Basell product, customers and other users should make their own independent determination that the product is suitable for the intended use. They should also ensure that they can use the Basell product safely and legally. (Material Safety Data Sheets are available from Basell at www.basell.com.) This document does not constitute a warranty, express or implied, including a warranty of merchantability or fitness for a particular purpose. No one is authorized to make such warranties or assume any liabilities on behalf of Basell except in a writing signed by an authorized Basell employee. Unless otherwise agreed in writing, the exclusive remedy for all claims is replacement of the product or refund of the purchase price at Basell's option, and in no event shall Basell be liable for special, consequential, incidental, punitive, or exemplary damages. Adflex, Adstif, Adsyl, Avant, Catalloy, Clyrell, Hifax, Higran, Histif, Hostacom, Hostalen, Hostalen PP, Hostalen ACP, Lucalen,Luflexen, Lupolen,Lupolex, Lupotech G, Lupotech T, Metocene, Moplen, Pro-fax, Pro-fax Ultra, Purell, Softell, Spherilene, Spheripol,Spherizone and Stretchene are trademarks owned or used by Basell. Adflex, Adstif, Adsyl, Clyrell, Hifax, Hostacom, Hostalen, Lucalen, Luflexen,Lupolen, Lupotech, Moplen and Pro-fax are registered in the U.S. Patent and trademark office. Unless specifically indicated, the grades mentioned are not suitable for applications in the pharmaceutical/medical sector Release Date: 17 Oct 2005