| TYRIL 790 ¦ SAN ¦ The Dow Chemical Company |  |
| --- | --- |

| Rheological properties | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Melt volume-flow rate | 28 | cm³/10min | ISO 1133 |  |
| Temperature | 220 | °C | ISO 1133 |  |
| Load | 10 | kg | ISO 1133 |  |

| Mechanical properties | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Tensile Modulus | 3800 | MPa | ISO 527-1/-2 |  |
| Yield stress | 76 | MPa | ISO 527-1/-2 |  |
| Yield strain | 2.6 | % | ISO 527-1/-2 |  |
| Nominal strain at break | 2.6 | % | ISO 527-1/-2 |  |
| Charpy impact strength (+23°C) | 17 | kJ/m² | ISO 179/1eU |  |
| Charpy impact strength (-30°C) | 18 | kJ/m² | ISO 179/1eU |  |
| Tensile notched impact strength (+23°C) | 17 | kJ/m² | ISO 8256/1 |  |

| Thermal properties | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Temp. of deflection under load (1.80 MPa) | 101 | °C | ISO 75-1/-2 |  |
| Vicat softening temperature (50°C/h 50N) | 101 | °C | ISO 306 |  |
| Coeff. of linear therm. expansion (parallel) | 0.5 | E-4/°C | ISO 11359-1/-2 |  |
| Coeff. of linear therm. expansion (normal) | 0.6 | E-4/°C | ISO 11359-1/-2 |  |
| Burning Behav. at 1.5 mm nom. thickn. | HB | class | IEC 60695-11-10 |  |
| Thickness tested | 1.5 | mm | IEC 60695-11-10 |  |
| UL recognition | UL | - | - |  |

| Electrical properties | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Relative permittivity (100Hz) | 2.8 | - | IEC 60250 |  |
| Relative permittivity (1 MHz) | 2.8 | - | IEC 60250 |  |
| Dissipation factor (100 Hz) | 0.8 | E-4 | IEC 60250 |  |
| Dissipation factor (1 MHz) | 1 | E-4 | IEC 60250 |  |
| Volume resistivity | >1E13 | Ohm*m | IEC 60093 |  |
| Surface resistivity | >1E15 | Ohm | IEC 60093 |  |

| Other properties | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Water absorption | 0.1 | % | Sim. to ISO 62 |  |
| Humidity absorption | 0.6 | % | Sim. to ISO 62 |  |
| Density | 1080 | kg/m³ | ISO 1183 |  |

| Material specific properties | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Viscosity number | 91 | cm³/g | ISO 307, 1157, 1628 |  |

| Rheological calculation properties | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Density of melt | 916 | kg/m³ | - |  |
| Thermal conductivity of melt | 0.148 | W/(m K) | - |  |
| Spec. heat capacity melt | 1870 | J/(kg K) | - |  |

| Test specimen production | Value | Unit | Test Standard |  |
| --- | --- | --- | --- | --- |
| ISO Data |  |
| Processing conditions acc. ISO | 4894 | - | ISO ....-2 |  |
| Injection Molding, melt temperature | 250 | °C | ISO 294 |  |
| mold temperature | 50 | °C | ISO 10724 |  |
| injection velocity | 300 | mm/s | ISO 294 |  |

Characteristic

Regional Availability

Europe